NUMER IDENTYFIKACYJNY // CONTRIBUTION ID
Magnetocaloric effect in antiferromagnetic EuCu2Sb2 compound
Karol Synoradzki1, Filip Krzyżanowski1, Tamara J. Bednarchuk2, Karol Załęski3, Dariusz Kaczorowski2
1 Institute of Molecular Physics of the Polish Academy of Sciences, Poznań, Poland
2 Institute of Low Temperature and Structure Research, Polish Academy of Sciences, Wrocław, Poland
3 NanoBioMedical Centre Adam Mickiewicz University, Poznań, Poland

Corresponding Author: karol.synoradzki@ifmpan.poznan.pl

Europium-based intermetallic compounds and alloys represent a fascinating class of materials, particularly due to the presence of divalent Eu2+ ions, which can give rise to a variety of magnetic and thermodynamic phenomena. Among these, the magnetocaloric effect (MCE) has attracted considerable attention, especially for applications in magnetic refrigeration at cryogenic temperatures. Some Eu-bearing compounds are among the most efficient known magnetocaloric materials in the low-temperature regime, making them highly relevant for fundamental studies and potential technological applications. In this study, we focus on the magnetocaloric properties of the antiferromagnetic intermetallic compound EuCu2Sb2, which crystallizes in the tetragonal CaBe2Ge2-type structure (space group P4/nmm, no. 129). Structural characterization confirms high quality of the polycrystalline sample, and magnetization measurements reveal an antiferromagnetic transition at 5.1(1) K. Electrical resistivity data indicate metallic-type electron transport, consistent with the behavior observed in similar Eu-based intermetallic systems. Magnetization isotherms were used to evaluate the magnetocaloric response of EuCu2Sb2. The compound exhibits both normal and inverse magnetocaloric effects, depending on temperature and field conditions. The maximum isothermal magnetic entropy change (–ΔSm) for the normal MCE reaches 13.2(1) Jkg-1K-1 near 6 K under an applied magnetic field change of 5 T. Additionally, the relative cooling power (RCP) is estimated to be 136(8) Jkg-1 for the same field variation. Our findings contribute to a deeper understanding of magnetocaloric behavior in Eu-based antiferromagnets and highlight EuCu2Sb2 as a potential candidate for cryogenic cooling technologies.

This study was supported by the National Science Centre (Poland) under grant 2021/41/B/ST3/01141.